08/01/2014

S565-14.docx

|  |
| --- |
| Include the following with projects requiring drilled shafts: |

## Section 565. — DRILLED SHAFTS

**Construction Requirements**

**565.08 Concrete for Drilled Shafts.** Delete the fourth paragraph and substitute the following:

Furnish concrete conforming to Section 552, except:

* Use Class C structural concrete having a slump of 7±1 inches (180±25 millimeters) for shafts constructed without drilling fluid;
* Use Class C structural concrete having a slump of 8±1 inches (200±25 millimeters) for shafts constructed with drilling fluid; and
* Seal concrete for under water placement.