*INCLUDE SECTION 615 AS NEEDED BASED ON CLAUSE INSTRUCTIONS*

$$615.00A

Section 615. — SIDEWALKS, PADS, AND PAVED MEDIANS

Revised 18 February 2016

*INCLUDE CLAUSES $$615.02A, $$615.03A, AND $$615.07A TO ALLOW THE USE OF CRUSHED RECYCLED CONCRETE- VERIFY WITH MATERIALS ENGINEER IF CLAUSES ARE APPROPRIATE TO USE (IF USED, ALSO INCLUDE CLAUSE $$703.18A)*

$$615.02A

615.02. Add the following:

Crushed recycled concrete 703.18

$$615.03A

615.03. Add the following:

Crushed recycled concrete may be used for bedding courses under sidewalks, pads, and paved medians. Place crushed recycled concrete according to the requirements of Subsection 302.04. Compact and finish crushed recycled concrete according to the requirements of Subsection 302.05, Method 1. Remove any layer of crushed recycled concrete material that exhibits heaving, pumping, rutting, or shearing under construction equipment even if the layer meets the compaction requirements of Subsection 302.05.

$$615.07A

615.07. Add the following:

Crushed recycled concrete material for aggregate courses under sidewalks, pads, and paved medians will be evaluated under Subsections 106.02 and 106.04.