08/26/2016

S705-14\_08262016.docx

|  |
| --- |
| Use on projects as appropriate. |

## Section 705. — ROCK

|  |
| --- |
| Use on projects gabions or revet mattresses |

**705.01 Gabion and Revet Mattress Rock.** Delete the following:

**(a)** Coarse durability index, AASHTO T 210 50 min.

|  |
| --- |
| Use on projects with rockeries |

**705.06 Rock for Rockeries.**  Delete the following:

**(d)** Coarse durability index, AASHTO T 210 52 min.

|  |
| --- |
| Use on projects with MSE walls or reinforced soil slopes. |

Add the following:

**705.08 Wall Facing Fill**.  Furnish hard, durable, angular rock that is free of organic or other unsuitable material. Angular rock is characterized by sharp, clean edges at the intersections of relatively flat surfaces. Do not use shale, rock with shale seams, or other fissile or fissured rock that may break into smaller pieces in the process of handling and placing. Conform to the following:

**(a)** Gradation. Furnish rock with breadth and thickness at least one-third its length with a 6 in (150 mm) maximum dimension. Ensure that 95 percent of wall facing fill particles minimum dimension exceeds welded wire facing opening with remaining 5 percent exceeding one-half welded wire facing opening.

**(b)** Soundness of aggregate using sodium sulfate, 15% loss max.

AASHTO T 104 (5 cycles)

**(c)** Los Angeles abrasion, AASHTO T 96 50% max.