11/05/2015

S725-14\_11052015.docx

|  |
| --- |
| Use on all projects. |

## Section 725. — MISCELLANEOUS MATERIAL

**725.04 Pozzolans.** Delete line (a) and substitute the following:

 **(a) Fly ash.** Conform to AASHTO M 295 4.5 percent max

 Class C or Class F.

 When used to mitigate alkali-silica reactivity,

 also available alkalies as equivalent Na2O