## Section 565. — drilled shafts

04/02/21–FP14

WFL Specification 04/02/21

Include the following when Drilled Shafts are required.

### 565.08 Concrete for Drilled Shafts..

Delete the fourth paragraph and substitute the following:

Furnish concrete conforming to Section 552, except:

* Class A (Drilled Shafts) structural concrete having a slump of 7±1 inches (180±25 millimeters) for shafts constructed without drilling fluid;
* Class A (Drilled Shafts) structural concrete having a slump of 8±1 inches (200±25 millimeters) for shafts constructed with drilling fluid; and
* Class S concrete for under water placement.