## Section 722. — ANCHOR MATERIAL

01/06/23 – FP-14

WFL Specification 01/06/23 7220010

Include the following when Section 256 work is required.

### 722.02 Anchor Tendons.

Delete Subsection (a) and substitute the following:

**(a) Prestressing steel.** Conform to one of the following:

**(1)** Stress-relieved steel wire for prestressed concrete ASTM A421

**(2)** Steel strand, low-relaxation, uncoated, seven-wire for concrete reinforcement AASHTO M 203

**(3)** Steel strand, seven-wire, uncoated, compacted for prestressed concrete ASTM A779

**(4)** High-strength steel bars for prestressed concrete AASHTO M 275

**(5)** Steel strand, low-relaxation, seven-wire for prestressed concrete ASTM A416